# Exercises KJM3110 Electrochemistry

Solutions are provided as Hidden text: File, Options, Display, Hidden text.

Solutions are provided as Hidden text: File, Options, Display, Hidden text.

## Chapter 5 Electrochemical power

A. We want to store 1 MJ of energy. How many Watt-hours Wh is that?

1 MJ = 106 J = 106 Ws = 106 Ws / 3600 s/h = 278 Wh

i) We consider to use an air-filled plate capacitor of plate distance 10 μm and charge it with 12 V. Sketch it. What capacitance do you need? How large area must it have?

E = QU = 106 J.   Q = 106 J / 12 V = 8333 F

C = Q/U = 8333 F / 12 V = 694 F

C = ε0εrA/l = 694 F.   A = C l/ε0εr ≈ C l/ε0 = 694 F 10*10-6 m / 8.85410-12 F/m = 7.83108 m2

ii) We consider instead to use a dielectric with relative dielectric constant εr = 1000 between the plates. Sketch it. What is the area needed now?

7.83105  m2

iii) You consider to use two capacitors of half this capacitance each. Will you connect them in series or parallel to get the required total capacitance? Sketch the circuit.

Parallel (Capacitances add in parallel)

iv) We consider instead to use a Li-ion secondary (rechargeable) battery. Sketch it. What is the specifications of the battery, the quantities of Li involved, a minimum weight of the battery, and assumptions made to get the required energy stored?The Li ion battery should have at least 278 Wh of energy, which at 4 V corresponds to a charge of 106 J / 4 V = 2.5∙105 F. This corresponds to 2.5∙105 F / 96485 C/mol = 2.6 mol Li. The weight of this Li is 2.6 mol x 6.94 g/mol = 18 g. However, there is at least one transition metal ion like Fe, 2 oxide ions, and 6 carbon atoms per Li, adding 2.6x(56 + 2x16 + 6x12) = 2.6 mol x 160 g/mol = 416 g. Other components (electrolyte, current collectors) also add. First estimate: 0.5 kg.

Batteries have losses during charging and discharging, depending on the rate. If we lose 10% each way, the numbers above must be multiplied accordingly (divided by 0.8).

v) We consider instead to store hydrogen and use it in a fuel cell. Sketch the storage and the fuel cell, after selecting a type of fuel cell so that you can use the proper ion and flows of reactants and products in the sketch. What is the specifications of the fuel cell, the quantities of hydrogen involved, a minimum weight of the system, and assumptions made to get the required energy stored?

Hints: The cell voltage is only ca. 1 V vs the 4 V of the Li ion battery. So you need 4 times more charges and hence moles of H. (2 times more moles of H2.) The weight of fuel is only 2.6 x 4 x 1 = 10.4 g H2, vs the > 0.5 kg of chemicals in the battery. Weight of tank and fuel cell and the efficiency of the system add, however.

B. The standard alkaline batteries have these two electrode reactions:

But alternative positive electrodes are:

For exercise and routine, write for each of the four batteries (combination of negative and positive electrode) the total reaction and the Nernst equation expression for the cell voltage.

Zn +HgO = ZnO + Hg(l)	E = E0

Zn + Ag2O = ZnO + 2Ag  	E = E0

Zn + 1/2O2(g) = ZnO		E = E0 – (RT/2F) ln(1/pO21/4)

C. Based on half-cell reactions in the textbook, write full cell reactions for Ni-Cd and Ni-H batteries. Write expressions for the Gibbs energy change for each.

Try yourself – use the textbook

D. The textbook suggests a fairly accurate set of reactions to describe the Li-ion battery using LiCoO2 and Li1/6C as, respectively, positive and negative electrodes in the discharged and charged states. Write simplified reactions and total reaction of the same assuming that the electrodes are empty or full of Li in the two states.

See lecture slide.

E. The Na-S battery has these electrode reactions:

Write the total reaction and cell voltage expression. Is this the equilibrium voltage? Open circuit voltage? Nernst voltage? Standard voltage? Operational voltage? Cut-off voltage?

Equilibrium voltage? Yes (local) or No (global)

Open circuit: Yes

Nernst: Yes

Standard: All reactants and products are condensed phases, so activities are 1, so Yes.

Operational voltage: No

Cut-off voltage? No

F. We use reforming and shift reactions to transform fossil fuels like methane (CH4) to CO2 and H2 as a fuel in fuel cells. Use Google to look up: What is steam reforming? Write the steam reforming reaction for CH4. What is the shift reaction? Write the total steam reforming plus shift reaction for CH4 to CO2 and H5. The reforming reaction is strongly endothermic. Why would we do it inside the fuel cell (internal reforming) rather than before the fuel cell (external reforming)?

CH4 + H2O = CO + 3H2 (reforming)

CO +H2O = CO2 + H2 (shift)

CH4 + 2H2O  CO2 + 4H2O (reforming  shift)

By doing this internally, the heat needed for the chemical reactions comes directly from the heat evolved by the electrochemical reaction. If we do it externally, we would need to transfer the heat from unit to another to utilize it.

G. Write half and full cell reactions as well as an expression for E and ΔG for fuel cells running on H2 and O2 for the different conducting ions in the following types of fuel cells: Alkaline, phosphoric acid or PEM, solid oxide, proton ceramic.

Hint: Use the same ion for both electrodes.

H. With reference to the slide with the figure to the right, in the case of a hydrogen fuel cell:

i) Let us look a bit closer at the heat exchange q. In a perfectly loss-free cell, it is given by TΔS. Explain.

ii) In a cell with losses, where do the additional contributions to q come from?

I. For the vanadium redox flow battery in the text book, the electrode reactions are

What is the total reaction and the expression for the voltage? What is the purpose and required properties of the membrane?